# Integrated Formulation Optimization: Methylene Blue Sustained-Release Tablets

## Optimization Target Review

The primary goal is to increase the **cumulative release amount** of the **Standard Formulation** (Medium Viscosity) during the first **4 hours** to **105%** of its current level. This requires a subtle shift in the matrix dynamics—specifically, a slight acceleration of the initial hydration and erosion rates without compromising the 24-hour sustained-release profile.

---

## Evidence Summary from Existing Formulations

* **Low-Viscosity Formulation (Too Fast):** The UV absorbance sum for the 0–4 h window is approximately **0.8930**, which is roughly **116%** of the standard formulation's level. Visually, the rapid loss of core geometry and early "blue burst" indicate that this HPMC ratio (approx. 1:4 K4M:100lv) provides insufficient diffusion resistance for the target.

* **High-Viscosity Formulation (Too Slow):** The UV absorbance sum for the 0–4 h window is approximately **0.6602**, which is only **86%** of the standard level. The video shows a very robust, sharp-edged core that resists erosion, confirming that the high K4M content (approx. 4:1 K4M:100lv) creates an overly restrictive barrier.

* **Standard Formulation (Reference):** With a 0–4 h UV sum of **0.7673**, this formulation serves as the baseline. Mechanistically, it maintains a stable gel "halo," but to reach the 105% target, the ratio must be shifted slightly toward the low-viscosity tendency to increase early-phase porosity and surface erosion.

---

## Recommended Next Formulation (Tentative)

This proposal is a best-estimate iteration based on a linear interpolation of the UV data and the observed mechanical transitions between the "Standard" and "Low-Viscosity" states.

* **Proposed HPMC K4M amount** = **2.0641**

* **Proposed HPMC 100lv amount** = **3.2536**

* **Proposed HPMC K4M:HPMC 100lv ratio** = **1 : 1.58**

* **Percentage change of HPMC K4M relative to the standard formulation** = **-17.56%**

* **Percentage change of HPMC 100lv relative to the standard formulation** = **+15.49%**

**Rationale:** The 5% increase target is modest. By reducing the K4M (high viscosity) by ~17.5% and increasing the 100lv (low viscosity) by ~15.5%, we decrease the polymer chain entanglement density in the initial gel layer. This modification is designed to allow the **"Swelling Front"** to penetrate the core slightly faster in the first 4 hours, mimicking the early-stage rounding seen in the low-viscosity video, while the remaining 2.06g of K4M ensures the "ghost" shell persists through the 24-hour mark.

---

## Uncertainty and Validation Needs

This formulation is **tentative** and subject to the following validation requirements:

1.  **Non-Linearity Correction:** Release rates in HPMC matrices often respond non-linearly to viscosity changes. A pilot batch is required to confirm if the -17.5%/+15.5% shift overshoots or undershoots the 105% target.

2.  **Total Polymer Mass:** This recommendation keeps the total HPMC mass nearly constant (~5.32g). If the 105% target is met but the 24-hour total release becomes too high, the total HPMC mass may need to be slightly increased in a subsequent step.

3.  **Mechanical Verification:** A texture analyzer should be used on this new iteration at the 4-hour mark to ensure the gel strength has decreased by the predicted margin compared to the Standard formulation.