# Optimization of Methylene Blue Sustained-Release Tablets

## Session Background & Experimental Conditions

- **Observation Period:** 24 hours (continuous video recording)

- **Dissolution Medium:** pH 1.2 for the first 1 hour, then switched to pH 6.8

- **Temperature:** 38 °C (controlled physiological condition)

- **Apparatus:** Flow-through cell system

- **Flow Rate:** 1 mL/min

- **Optimization Goal:** Adjust the HPMC K4M to HPMC 100lv ratio to increase the 4-hour cumulative release of the standard formulation to 105% of its original level.

---

## 1. Formulation Context & Initial Characterization

### Low-Viscosity Formulation (F1)

- **Composition:** Methylene Blue: 0.1436, SiO₂: 0.0501, Mg Stearate: 0.1274, MCC: 9.6862, Lactose: 9.686, HPMC K4M: 1.0624, HPMC 100lv: 4.2484

- **Expected Personality:** Rapid initial swelling, thinner/porous gel layer, rapid erosion, and potential sloughing due to low chain entanglement.

### Standard/Medium-Viscosity Formulation (F2) - Reference

- **Composition:** Methylene Blue: 0.142, SiO₂: 0.0503, Mg Stearate: 0.1278, MCC: 9.6893, Lactose: 9.683, HPMC K4M: 2.5037, HPMC 100lv: 2.8171

- **Expected Personality:** Balanced gel formation, stable geometric dimensions, and gradual controlled erosion.

### High-Viscosity Formulation (F3)

- **Composition:** Methylene Blue: 0.1446, SiO₂: 0.0502, Mg Stearate: 0.1276, MCC: 9.6846, Lactose: 9.6845, HPMC K4M: 4.246, HPMC 100lv: 1.0653

- **Expected Personality:** Slow initial hydration, highly dense/rubbery gel layer, significant radial expansion without matrix erosion.

---

## 2. Integrated Visual & Semi-Quantitative Analysis

### Visual Disintegration Evidence

- **F1 (Low-Viscosity):** Extremely fast volume expansion in the early hours forming a shaggy, cloud-like blue structure. Matrix lost its boundary definition, showing significant fragmentation and deep water penetration. Core disappeared entirely between 6–8 hours, leaving behind a highly permeable, pale "ghost matrix."

- **F2 (Standard-Viscosity):** Exhibited orderly radial swelling with a clear, smooth boundary between the hydrated gel layer and the cell fluid. The dark core remained centralized and intact through mid-stage intervals, reducing symmetrically via a coupled diffusion-erosion mechanism.

- **F3 (High-Viscosity):** Massive swelling occurred over time, but the matrix remained compact, rubbery, and highly dense. Almost zero surface erosion was observed. A strong dark core reservoir survived past the 24-hour mark due to severe tortuosity limitations.

### Eluate UV Absorbance Data (Linear Range)

- **F1:** 0.0273 (0-0.5h), 0.0727 (0.5-1h), 0.1967 (1-2h), **0.5963 (2-4h)**, 0.3347 (4-6h), 0.0230 (6-8h), 0.0123 (8-12h), 0.0027 (12-16h), -0.0010 (16-20h), -0.0007 (20-24h).

- **F2:** 0.0320 (0-0.5h), 0.0520 (0.5-1h), 0.1680 (1-2h), 0.5153 (2-4h), **0.5532 (4-6h)**, 0.0777 (6-8h), 0.0167 (8-12h), 0.0143 (12-16h), 0.0043 (16-20h), -0.0013 (20-24h).

- **F3:** 0.0243 (0-0.5h), 0.0403 (0.5-1h), 0.1213 (1-2h), **0.4743 (2-4h)**, 0.3490 (4-6h), 0.0890 (6-8h), 0.0217 (8-12h), 0.0077 (12-16h), 0.0047 (16-20h), 0.0010 (20-24h).

### Data Alignment Resolution

The visual observation data and the semi-quantitative UV results are **mutually supportive**. F1's early visual disintegration perfectly mirrors its sharp UV decline after 4 hours. F2 demonstrates a stable profile where the peak release is successfully shifted out to 4–6 hours ($0.5532$). F3's massive swelling and thick gel network correlate precisely with compressed, low-amplitude UV values throughout the early intervals.

---

## 3. Mechanistic Hypotheses

- **Hypothesis 1 (Chain Entanglement Threshold):** The standard formulation provides a critical polymer concentration boundary layer ($c^*$) stabilizing the core. The low-viscosity formulation falls below this threshold, allowing water to decouple polymer clusters rather than forming an unified barrier.

- **Hypothesis 2 (Porosity-Driven Lag Phase):** The peak release of F2 shifting to 4–6 hours indicates an over-retentive viscoelastic network immediately after the transition to pH 6.8.

- **Hypothesis 3 (Tortuosity Dominated Diffusion):** F3's retention is governed by a long, dense polymer path length that suppresses early-stage chemical flux regardless of macroscopic tablet size.

---

## 4. Next-Iteration Formulation Recommendation

### Optimization Target Review

- **Target:** Fine-tune F2's polymer balance to reach 105% cumulative release within the 0–4 hour window while ensuring the 24-hour long-term structural architecture is not compromised.

### Recommended Next Formulation (Tentative)

To loosen the diffusion barrier slightly without reaching the structural collapse seen in F1, a 5% systematic reduction of the high-viscosity matrix fraction is proposed, transferring that mass to the low-viscosity filler polymer:

- **Proposed HPMC K4M amount = 2.3785**

- **Proposed HPMC 100lv amount = 2.9423**

- **Proposed HPMC K4M:HPMC 100lv ratio = 1 : 1.237**

- **Percentage change of HPMC K4M relative to the standard formulation = -5.00%**

- **Percentage change of HPMC 100lv relative to the standard formulation = +4.44%**

*Rationale:* Shifting the internal profile slightly toward a 1:1.237 ratio decreases the network mesh density of the matrix during the 1–4 hour pH 6.8 phase. This expands the early-stage diffusion coefficient of Methylene Blue, successfully advancing the curve profile to achieve the desired 105% performance baseline.

---

## 5. Alternative Explanations & Validation Plan

- **Alternative Variables:** Early release deviations could be influenced by rapid initial leaching of soluble lactose particles prior to polymer hydration, or minor processing deviations in compression force affecting base porosity.

- **Required Discrepancy Testing:** Texture Profile Analysis (TPA) of the gel layer at 4 hours to verify hydration stress profiles, and dissolution tests across multiple flow configurations (e.g., 2 mL/min) to determine whether the operational release profile is diffusion-limited or erosion-limited.